## Slide 1: Mirror coatings for EUV and soft X-Ray imaging
David D. Allred -BYU
BYU EUV Optics
Jan. 4, 2020
Notes: IMAGE was the first satellite mission dedicated to imaging the Earth's magnetosphere, the region of space controlled by the Earth's magnetic field and containing extremely tenuous plasmas of both solar and terrestrial origin. Invisible to standard astronomical observing techniques, these populations of ions and electrons have traditionally been studied by means of localized measurements with charged particle detectors, magnetometers, and electric field instruments. Instead of such in-situ measurements, IMAGE employs a variety of imaging techniques to "see the invisible" and to produce the first comprehensive global images of the plasma populations in the inner magnetosphere. With these images, space scientists are able to observe, in a way never before possible, the large-scale dynamics of the magnetosphere and the interactions among its constituent plasma populations.
http://pluto.space.swri.edu/IMAGE/

## Slide 2: Our group has made spaces mirrors for Far, Extreme Ultraviolet (EUV)
Thin Film or Multilayer Mirrors
EUV Astronomy
The Earth’s magnetosphere in the EUV-30.4 nm
BYU EUV Optics
Jan. 4, 2020
IMAGE spacecraft- NASA midex mission to Earth. ~2000
Imager for Magnetopause to Aurora global explorer.
EUV Instrument –
He+ trapped in Earth’s magnetosphere scatters EUV-30.4 nm
http://pluto.space.swri.edu/IMAGE/
Google: EUV LPL
(more info: Sandel, B. R., et al., Space Sci. Rev., 109, 25, 2003.)
Please give us your hard thin-film optics fabrication problems. They are very good for our students.
Notes: [Talk a lot about applications.]
***[Click]***
Extreme Ultraviolet optics have applications in many varied fields.
***[Click]***
For example, Ultraviolet optics are often used in astronomical observations. BYU currently has a uranium thin film mirror on the IMAGE satellite. This picture of the earth’s magnetosphere was taken in the EUV with the optics on board the IMAGE satellite.
***[Click]***
In addition, EUV optics may soon be of great benefit to the micro-processing industry. Current computer chips are made with deep ultraviolet wavelengths of light. This corresponds to a resolution of several hundred nanometers. These current methods are reaching an effective barrier, and microprocessor manufacturers will have to switch to reflective EUV and soft X-Ray optics within the next couple of years. Lithography at the wavelengths with which we are dealing could dramatically decrease the size of computer chip features.
***[Click]***
Future applications may include soft X-Ray [about 4 nm “water window”] microscopes. Current cellular microscopes rely on coating the specimens with gold atoms and studying the structure with a tunneling electron microscope. Since the gold coating process is lethal to microorganisms, this only gives an image of the organism after it has been dead for quite some time. EUV microscopes, while also potentially lethal to microorganisms, would give a much clearer view of the living cellular structure of the specimen.

## Slide 3: Effects of The Atmosphere on the Electromagnetic waves
http://www.wikiwand.com/en/Electromagnetic_radiation
Space mirrors because: Only part of the electromagnetic spectrum gets through the atmosphere.
Notes: UV is from 100-400nm

## Slide 4: Three ways of getting mirrors. Plasma, low-angle reflectance & … While no solid barrier layer is transparent below ~103nm, simulations show
Of all reflectors aluminum
has lowest λ plasma edge

## Slide 5: Obtaining High reflectance in EUV & x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
2. Low angle
reflectance is high.
Wolter
3. Multilayer reflectance
BYU EUV Optics
Jan. 4, 2020
By Andreas 9384 - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=54729753

## Slide 6
http://physics.stackexchange.com/questions/216302/interference-of-light-in-a-dielectric-mirror
http://www.dichroic.com.tw/dielectric.htm
Reflectance is proportional to amplitude squared.
Two ways of getting mirrors.
Plasma & ML

## Slide 7: Mo/Si & Mo/Be ML are champions
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
BYU EUV Optics
Jan. 4, 2020
https://www.rigakuoptics.com/euv.php
Cross-sectional TEM image of a 40-pair Mo/Si ML mask blank.
R (near normal)> 70% wavelength
~11 to 14 nm
many space-based solar observatories
<70 layer pairs each about 7nm
Total thickness < <1μm
Smoothing
SOA: Market pull
EUV Microlithography
Optical Elements
Size: Up to 1 m
Figure: to 0.1nm
Roughness <0.2nm
Many refinements
https://www.researchgate.net/publication/253883863_Masks_for_extreme_ultraviolet_lithography/figures?lo=1
Manufacturers:
inhouse EUVL tool
Ovonyx
researchers: R. Soufli,
F. Delmotte, D. Windt, BYU

## Slide 8: Our group has made “space” mirrors for Far, Extreme Ultraviolet (EUV)
Thin Film or Multilayer Mirrors
BYU EUV Optics
Jan. 4, 2020
EUV Instrument –
What might we see in Jupiter’s magnetosphere?
EUV
LPL UofAz
(From Sandel, B. R., et al., Space Sci. Rev., 109, 25, 2003.)
U/Si ML 12.5 periods
U on (bottom and U on top.
R=16% @30.4 nm
Top U was an AR layer for 58.4 nm
(He-I) 8 mirrors,
“highly curved” f~1.5
3 flew .
As it tumbled mapped out 3π
made movies.
Take home perspectives:
  1. ML means not broad.
  2. Absorption – Refl. peak not tall. >50%
  3. possible over most of EUV
  4. Dual function mirrors are possible
Notes: [Talk a lot about applications.]
***[Click]***
Extreme Ultraviolet optics have applications in many varied fields.
***[Click]***
For example, Ultraviolet optics are often used in astronomical observations. BYU currently has a uranium thin film mirror on the IMAGE satellite. This picture of the earth’s magnetosphere was taken in the EUV with the optics on board the IMAGE satellite.
***[Click]***
In addition, EUV optics may soon be of great benefit to the micro-processing industry. Current computer chips are made with deep ultraviolet wavelengths of light. This corresponds to a resolution of several hundred nanometers. These current methods are reaching an effective barrier, and microprocessor manufacturers will have to switch to reflective EUV and soft X-Ray optics within the next couple of years. Lithography at the wavelengths with which we are dealing could dramatically decrease the size of computer chip features.
***[Click]***
Future applications may include soft X-Ray [about 4 nm “water window”] microscopes. Current cellular microscopes rely on coating the specimens with gold atoms and studying the structure with a tunneling electron microscope. Since the gold coating process is lethal to microorganisms, this only gives an image of the organism after it has been dead for quite some time. EUV microscopes, while also potentially lethal to microorganisms, would give a much clearer view of the living cellular structure of the specimen.

## Slide 9: Are EUV and soft x-ray good areas for cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020
YES!

## Slide 10: Future opportunities for cube sats: 1. Bare Aluminum
Aluminum
IR on left Visible UV Far UV
Effect of Aluminum oxide
Effect of Fluoride (MgF2 etc.) over coat.
Bare Al - high reflectance to the Lyman break.
Yes. Evaporate Al is possible.

## Slide 11: Future opportunities for cube sats: 2. GET high reflectance to 20eV 60nm Bare Aluminum on a EUV mirror
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Concept
2. how?
Bare Al on EUV ML centered at ~80nm
Note the peak at 72 nm
Interference peak
Al “transparent” below plasma edge.
BYU EUV Optics
Jan. 4, 2020

## Slide 12: Future opportunities: EUV or soft x-ray ML on bare Al mirror While no solid barrier layer is transparent below ~103nm, simulations show
Logistic:
Have a ML mirror(s) on telescope surfaces.
Coat thin Al (~42 nm) in space.

## Slide 13
EUV mirror under an Al coating?
Peak in EUV- for example:
30.4 nm
Example 1: An exploratory design of
wide VUV-EUV & high 30 nm reflectance
Genetic Algorithm employed

## Slide 14: An exploratory design of wide VUV-EUV & 20 nm- computed
Pioneering stage- more constants are needed.
Collaboration between those doing measurements & fabrication would help.

## Slide 15: Could we reliably aluminize surfaces in space?
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
We would like to help you coat your cube mirrors and gratings with EUV/soft x-ray function.
Whether it be standard or more challenging
such as the bare aluminum on EUV mirrors.
BYU EUV Optics
Jan. 4, 2020
Evaporator with self contained power- Zecoat. David Sheikh,

## Slide 16: Allred- Turley –XUV-thin film Research Group
Steven Turley back from NSF 2-year appointment in education branch.
Acknowledge: financial support of the College of physical and mathematical sciences-BYU, the Utah NASA space grant consortium and the NSF-REU program.
Our group loves designing, Fabricating, testing, understanding optical thin-films, and problems with and fixing them. Please give us your hard fabrication problems. They are very good for our students.

## Slide 17: History of All Sky EUV & Far UV
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
EUVE 7-70nm June 1992 to Jan, 2001. ROSAT WFC and EUVE missions
    Typical effective areas for the survey instruments ranged from ≈10–20 cm2, glancing angle
FUSE 90.5 to 119.5 nm; June 99- Oct. 07-
    4 near normal mirrors each about 39-by-35 cm (15.4-by-13.8 in) off-axis parabola
Galex 135–280 nm (Far Ultraviolet)
Hubble COS – has FUV 90-205 nm
NO EUV at present
BYU EUV Optics
Jan. 4, 2020

## Slide 18: Cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020

## Slide 19: Are Cube and Small Sats an answer to an EUV astronomers’ plea?
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
“The principal limitation is the absorption by the interstellar medium that defines the horizon within which sources can be observed. …
“Therefore, … EUV observations are … mostly restricted to a local region of our galaxy.
“… it may never be possible to justify an expenditure on future missions similar to the large X-ray or UV observatories.” Martin A. Barstow in
chapter “EUV astronomy in the 21st century,” of Extreme Ultraviolet astronomy. By Martin A. Barstow.
BYU EUV Optics
Jan. 4, 2020
Applications? where understanding what is happening in local region of the galaxy may be important?
Planets in our own solar system?
Environment of extrasolar planets?
CUTE
Potential of Cubesat?
https://gnuva.net/gnuva_barstowbio.htm
Scattering/Absorption situation:
Notes: The Colorado Ultraviolet Transit Experiment (CUTE): A dedicated cubesat mission to study exoplanetary mass loss and magnetic fields
Brian T. Fleming, Kevin France, Nicholas Nell, Richard Kohnert, Kelsey Pool, Arika Egan, Luca Fossati, Tommi Koskinen, Aline A. Vidotto, Keri Hoadley, Jean-Michel Desert, Matthew Beasley, Pascal Petit
(Submitted on 8 Jan 2018)
The Colorado Ultraviolet Transit Experiment (CUTE) is a near-UV (2550 - 3300 Angstrom) 6U cubesat mission designed to monitor transiting hot Jupiters to quantify their atmospheric mass loss and magnetic fields. CUTE will probe both atomic (Mg and Fe) and molecular (OH) lines for evidence of enhanced transit absorption, and to search for evidence of early ingress due to bow shocks ahead of the planet's orbital motion. As a dedicated mission, CUTE will observe more than 100 spectroscopic transits of hot Jupiters over a nominal seven month mission. This represents the equivalent of more than 700 orbits of the only other instrument capable of these measurements, the Hubble Space Telescope. CUTE efficiently utilizes the available cubesat volume by means of an innovative optical design to achieve a projected effective area of 28 sq. cm, low instrumental background, and a spectral resolving power of 3000 over the primary science bandpass. These performance characteristics enable CUTE to discern transit depths between 0.1 - 1% in individual spectral absorption lines. We present the CUTE optical and mechanical design, a summary of the science motivation and expected results, and an overview of the projected fabrication, calibration and launch timeline. https://arxiv.org/abs/1801.02673

## Slide 20: Cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020

## Slide 21: Past Applications & new opportunities
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Solar system and beyond
  Moon
  Planetary- Jupiter
    S-L comet collision*
    Magnetosphere The Io torus –”many emissions of sulfur, oxygen, and even sodium ions at wavelengths between 35 and 75 nm.”
  20 years since EUVE- No current missions
When Hubble stops working? What then for far UV?
BYU EUV Optics
Jan. 4, 2020
*EUVE Observations of Jupiter During the Impact of Comet Shoemaker-Levy 9
G. Randall Gladstone1, Doyle T. Hall2, J. Hunter Waite Jr., Science 16 Jun 1995, Vol. 268, Issue 5217, pp. 1595-1597- DOI: 10.1126/science.268.5217.1595
https://solarsystem.nasa.gov/resources/11663/jupiters-magnetosphere/
Notes: he Atmospheric Imaging Assembly (AIA) instrument onboard the Solar Dynamics Observatory (SDO) is an array of four normal-incidence reflecting telescopes that image the Sun in ten EUV and UV wavelength channels. We present the initial photometric calibration of AIA, based on preflight measurements of the response of the telescope components. The estimated accuracy is of order 25%, which is consistent with the results of comparisons with full-disk irradiance measurements and spectral models. We also describe the characterization of the instrument performance, including image resolution, alignment, camera-system gain, flat-fielding, and data compression.

## Slide 22: Cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020

## Slide 23: Aperture considerations- Cube sats may not be too small
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
w Grazing angle
ROSAT WFC and EUVE missions
Typical effective areas for the survey instruments ranged from ≈10–20 cm2, while the peak effective area of the EUVE spectrometer was ≈1 cm2.
Near normal incidence- ML
20 cm aperture telescopes are on the Atmospheric Imaging Assembly (AIA) instrument aboard NASA's Solar Dynamics Observatory (SDO)– “Using SiC for Lightweight EUV Space Optics,” Martinez-Galarce, Dennis S.; et al. https://ui.adsabs.harvard.edu/abs/2009SPD....41.1813M/abstract
Cube Sat / 10 cm aperture?
BYU EUV Optics
Jan. 4, 2020
Notes: Although the ROSAT WFC and EUVE missions can be claimed as outstanding successes,
their telescopes were of comparatively limited aperture. Typical effective areas for the survey
instruments ranged from ≈10–20 cm2, while the peak effective area of the EUVE spectrometer
was ≈1 cm2. These figures can be contrasted with the >200 cm2 effective area of the
ROSAT XRT with its PSPC detector. Clearly, it would be desirable to construct new EUV
instrumentation with much higher effective areas than already flown.

## Slide 24: Cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020

## Slide 25: Solar opportunities?
Nano flares?

## Slide 26
https://solarsystem.nasa.gov/resources/11663/jupiters-magnetosphere/

## Slide 27: Current Applications EUV are solar
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Solar
  SOHO, STEREO
BYU EUV Optics
Jan. 4, 2020
  SDO | Solar Dynamics Observatory-
  4 Normal incidence telescopes
    multiple MLs
    10 EUV and UV channels
https://sdo.gsfc.nasa.gov/mission/instruments.php
Notes: he Atmospheric Imaging Assembly (AIA) instrument onboard the Solar Dynamics Observatory (SDO) is an array of four normal-incidence reflecting telescopes that image the Sun in ten EUV and UV wavelength channels. We present the initial photometric calibration of AIA, based on preflight measurements of the response of the telescope components. The estimated accuracy is of order 25%, which is consistent with the results of comparisons with full-disk irradiance measurements and spectral models. We also describe the characterization of the instrument performance, including image resolution, alignment, camera-system gain, flat-fielding, and data compression.

## Slide 28: Cube sat applications for EUV and soft x-ray
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Yes
No all sky observatory now
  Provide long time baseline
Lots of interesting problems locally
  Solar system – Jupiter,
  how about looking at exoplanet environment.
Aperture comparable to Past missions
Cube sat observatory dedicated to one or few task
Technology:
  Has advanced and
  May advance technology readiness level.
May be not there
EUVE did all sky survey
Absorption  EUV is a “niche” tool
Such as?
  Limited to local region of galaxy
Small aperture
Hubble exists
BYU EUV Optics
Jan. 4, 2020

## Slide 29: Extras follow:

## Slide 30: Two ways of getting mirrors. Reflector
Aluminum
IR on left Visible UV Far UV
Effect of Aluminum oxide
Effect of Fluoride (MgF2 etc.) over coat.
When reflectance falls Al begins to transmit. Could there be a multilayer reflector to give you a broader reflector?

## Slide 31: Two issues- Scattering of light from rough surface & protecting Aluminum for oxidation to reach far UV
Aluminum
IR on left Visible UV Far UV
Effect of Aluminum oxide
Effect of Fluoride (MgF2 etc.) over coat.
When reflectance falls Al begins to transmit. Could there be a multilayer reflector to give you a broader reflector?

## Slide 32
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
BYU EUV Optics
Jan. 4, 2020

## Slide 33: Multilayer mirrors for EUV & soft x-ray reflectors and gratings
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Light interacts strongly with matter
No solid material is entirely transparent < 100 nm
λ < Al plasma Edge
ML
EUV over stellar distances.
BYU EUV Optics
Jan. 4, 2020
Notes: may be scattered or absorbed.

## Slide 34: Multilayer mirrors for EUV & soft x-ray reflectors and gratings
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Light interacts strongly with matter
No solid material is entirely transparent < 100 nm
λ < Al plasma Edge
ML
EUV over interstellar distances.
BYU EUV Optics
Jan. 4, 2020
Notes: may be scattered or absorbed.

## Slide 35: Some potential targets: think of EUV Explorer, FUSE & Galex
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
Solar system
  Sun-
  Jupiter & its moon’s
Return to Extrasolar
  Since 2001
BYU EUV Optics
Jan. 4, 2020
Notes: EUVU 7-70nm June 1992 to jan, 2001.
FUSE 90.5 to 119.5 nm near normal mirrors

## Slide 36: Our goal is doubling* the effective bandwidth in space mirrors and gratings etc.
A multilayer VUV-EUV mirror below a thin (oxide-free) Al film
Common ground?
1. Understand corrosion under Barriers
2. Developing Barrier layers- Ultrathin & Engineered ML
3. Removable barrier layers is focus-
*From current 0 to ~10 eV to 0 to ~20 eV or 0 to 15 + another 5eV further on in EUV, such as 40-42eV & 47-49 eV or 60-70 eV
Notes: Our goal is to create and provide knowledge to those who will be making decisions about how a doubling* the effective bandwidth for aluminum mirrors might be achieved.
Advance the technology readiness level for using bare aluminum mirrors and bare aluminum mirrors with EUV reflectance to and, for some, through TRL 3.

## Slide 37
Motivation for Research
What is Hubble’s replacement for the UV community?
“LUVOIR”
photo credit: NASA
The concept design of the LUVOIR space telescope at the L2 Lagrange point with its 15.1-meter primary mirror Image credit: NASA / LUVOIR concept team; Serge Brunier (background).
Notes: In 2020 in their next decadal survey, NASA will be considering for priority a new space telescope called LUVOIR. It’s called LUVOIR because it wil be large and will collect information in the ultraviolet, optical, and infrared wavelength ranges. The mirror for this telescope – which will be 8-16 meters in diameter – will need to be coated with an excellent broadband reflector.
This is an image of the James Webb telescope – which had a 6.5 m diameter mirror . You can see in the picture how big that is compared to the people working on it. LUVOIR wil be even bigger.

## Slide 38
Cube Sat Workshop- 235th AAS meeting Honolulu Hawaii-4 Jan. 2020
BYU EUV Optics
Jan. 4, 2020